## Slide 1: MICROWAVE TRANSISTORS

## Slide 2: MICROWAVE SOLID-STATE DEVICES

## Slide 3: MICROWAVE BIPOLAR TRANSISTORS
For microwave applications, the silicon (Si) bipolar transistors dominate for frequency range from UHF to about S band (about 3 GHz).
As the technology improves, the upper frequency limit for these devices is continuously being extended,
and at the present time the devices are capable of producing useful power up to22 GHz.

## Slide 4: Physical Structures-BJT
All microwave transistors are now planar in form and almost all are of the silicon n-p-n type.
The geometry can be characterized as follows: (a) interdigitated, (b) overlay, and (c) matrix (also called mesh or emitter grid) as shown in Fig.
For high-frequency applications, the n-p-n structure is preferred because the electron mobility (μ n = 1500 cm2/V •s) is much higher than the hole mobility(μp =450 cm2/V •s). Figure shows an example of the densities for an n-p-n transistor. The density unit is in cm2/V •s.

## Slide 5: Construction of Microwave Transistors
An n type epitaxial layer is grown on n+ substrate that constitutes the collector. On this n region, a SiO2 layer is grown thermally. A p-base and heavily doped n-emitters are diffused into the base. Openings are made in Oxide for Ohmic contacts. Connections are made in parallel.
Such transistors have a surface geometry categorized as either interdigitated, overlay, or matrix. These forms are shown in the following figure
Power transistors employ all the three surface geometries.
Small signal transistors employ interdigitated surface geometry. Interdigitated structure is suitable for small signal applications in the L, S, and C bands.
The matrix geometry is sometimes called mesh or emitter grid. Overlay and Matrix structures are useful as power devices in the UHF and VHF regions.

## Slide 6: Operation of Microwave Transistors
n a microwave transistor, initially the emitter-base and collector-base junctions are reverse biased.
On the application of a microwave signal, the emitter-base junction becomes forward biased.
If a p-n-p transistor is considered, the application of positive peak of signal, forward biases the emitter-base junction, making the holes to drift to the thin negative base.
The holes further accelerate to the negative terminal of the bias voltage between the collector and the base terminals. A load connected at the collector, receives a current pulse.

## Slide 7
CB CONFIGURATION
CE CONFIGURATION

## Slide 8: FET

## Slide 9: Metal-Semiconductor Field Effect Transistor (MESFETs)
The Metal-Semiconductor-Field-Effect-Transistor (MESFET) consists of a conducting channel positioned between a source and drain contact region as shown in the Figure .
The carrier flow from source to drain is controlled by a Schottky metal gate.
The control of the channel is obtained by varying the depletion layer width underneath the metal contact which modulates the thickness of the conducting channel and thereby the current between source and drain
The higher transit frequency of the MESFET makes it particularly of interest for microwave circuits.
While the advantage of the MESFET provides a superior microwave amplifier or circuit, the limitation by the diode turn-on is easily tolerated.
Typically depletion-mode devices are used since they provide a larger current and larger transconductance and the circuits contain only a few transistors, so that threshold control is not a limiting factor.
The buried channel also yields a better noise performance as trapping and release of carriers into and from surface states and defects is eliminated.

## Slide 10: MESFET
The use of GaAs rather than silicon MESFETs provides two more significant advantages:
first, the electron mobility at room temperature is more than 5 times larger, while the peak electron velocity is about twice that of silicon.
Second, it is possible to fabricate semi-insulating (SI) GaAs substrates, which eliminates the problem of absorbing microwave power in the substrate due to free carrier absorption.